## Slide 1: Presentation at Hisense Photonics
Yuchao Jiang, PhD
2018.12.10

## Slide 2: Outline
Educational background
Past research experience
A detour in career
What I can do for HiSense Photonics

## Slide 3: Educational Background
Born in FuJian(福建).
2007, B.S., Applied Physics.
2010. M.S., Material Physics.
2016. Ph.D. in Electrical & Computer Engineering.

## Slide 4: My research experience
InP-based Quantum Cascade (QC) Lasers
  Surface-emitting DFB QC lasers at λ ~ 4.6 µm
InAs-based Interband Cascade (IC) lasers
  Single-mode DFB IC laser at λ=4.5 μm
  CW operation above RT at λ=4.6-4.8 μm
  Pulsed operation above RT at λ=6.2-6.7 μm
  Electrically widely tunable IC laser near λ=7 μm
GaSb-based type-I IC lasers
  CW operation above RT at λ=3.2 μm

## Slide 5: Why interband cascade (IC) lasers?
Mid-IR: 3-8 μm; Long-IR: 8~15 μm
Applications:
Gas-sensing
(ppb-level trace gas)
Free space optical communications
Highly energy efficient! 1/10 of competitor (QC laser).
Using iPhone 6 battery (10.5 Wh) can work ~50 hours.
Launch: 2011.11.26
Landing: 2012.8.6

## Slide 6: Methane on Mars? No?
One year after landing…
Notes: Sensing methane is difficult

## Slide 7: Methane on Mars? Yes!
Another year passes…
1 Mars year = 687 earth days
1 Mars day = 1 earth day + 41 min
Notes: https://mars.nasa.gov/allaboutmars/facts/#?c=inspace&s=distance

## Slide 8: Why interband cascade (IC) lasers? vs. non-cascade interband lasers
Shared issues for any interband lasers:
free carrier absorption loss
Auger recombination dominates Jth(=e∙nth/ τ)
Advantages of cascade structure :
reduce nth-> reduce Auger
Analogy: power transmission line -> lower ohmic loss
R. Yang, S. Pei, J. Appl. Phys. 79,8197(1996)
 | type | equivalent circuit | key difference
a | MQW laser | in parallel | low voltage
b | IC laser | in series | low current
GaN LED in a cascade structure overcame efficiency droop.
F. Akyol, et al., Appl. Phys. Lett. 103,081107(2013)

## Slide 9: Why interband cascade (IC) lasers? vs. quantum cascade (QC) lasers
Only two technologies capable of CW RT in mid-IR
 | QC laser | IC laser
material system | InGaAs/InAlAs/InP | InAs/GaSb/AlSb
carrier transition, lifetime | inter-subband, ~1 ps | interband, ~1 ns
threshold current density | 860 A/cm2 @4.6μm | 100 A/cm2 @3.6μm
threshold voltage | 12.8 V (40 stages) | 3 V (10 stages)
threshold power density | 11 kW/cm2 | 0.3 kW/cm2
maximum output power | 5.1 W | 0.6 W
thermal conductivity | InP: 68 W/m∙K | GaSb:33; InAs:27
IC laser is a better solution for battery powered applications.
ref: APL, 95,141113 (2009) ; APL, 102,231123(2013)
APL, 89,181102 (2011); Opt Exp., 22,7702(2014)

## Slide 10: Snapshot of IC laser development
How the progress is made?
better material & fabrication
improved understanding & design
trial and error

## Slide 11: Real device & testing set-up
Cascade stages
Top spacer
Bottom spacer
1 μm
Side
view
200 μm
Laser mesa
Trench
Cryostat
sensor A
Vacuum
LN2
Temperature
Controller
sensor B
heater
Laser
Current in
Light
out
Semiconductor grating

## Slide 12: InAs-based Single-mode DFB IC laser
Single frequency-mode laser is desirable for gas-sensing
First DFB IC laser with an asymmetric waveguide
Y. Jiang, et al., IEEE J. Quantum Electron. 51, 2300307(2015)

## Slide 13: Laser design for lowering Jth(T)
Modal gain (measurable)
Confinement factor
of Active QWs
Material gain (unmeasurable)
End goal: minimize threshold:
Design approaches:
Active core optimization
Optical waveguide optimization

## Slide 14: Band structure of IC laser
“Rebalancing of internally generated carriers for mid-infrared interband cascade lasers with very low power consumption”,
Vurgaftman, et al., Nature Communication, 2, 585 (2011)
bias
Design innovations since the prototype by R. Yang in 1994:
“W” like active region
2 QWs in hole injector
fine tune barrier thickness
semi-metallic interface
shortened electron injector
“carrier rebalancing”
(not fully understood)

## Slide 15: Waveguide structures of IC lasers
Material | Thermal Conductivity
InAs/AlSb SL | ~ 2.7 W/m·K
InAs | ~ 27 W/m·K
GaSb | ~ 33 W/m·K
Better thermal dissipation
Simplify the growth
Tunable refractive index
GaSb Substrate
GaSb Spacer
Cascade Stages
InAs/AlSb SL n=3.35
GaSb Spacer
InAs/AlSb SL
Contact
n=3.45
n=3.73
InAs Substrate
InAs Spacer
Cascade Stages
InAs n++ n~3
InAs Spacer
InAs n++
Contact
n=3.45
n=3.49
InAs-based IC lasers may be
a better solution at longer λ
top cladding
bottom
cladding
InAs Plasmon-Enhanced Waveguide
InAs/AlSb Superlattice Waveguide

## Slide 16: Optical waveguide optimization(1)
plasmon
frequency
doping
concentration
Drude model
When λemission near λplasmon:
n decreases sharply
loss increase exponentially

## Slide 17: Optical waveguide optimization(2)
Plasmon waveguide
requires higher
material gain!

## Slide 18: Optical waveguide optimization(3)
Hybrid waveguide:
InAs spacer layer
InAs/AlSb SL inner cladding
InAs plasmon outer cladding
Predict threshold gain
reduced by ~30%

## Slide 19: CW RT operation at λ=4.6-4.8 μm (1)
Max pulsed operation
temperature: 377 K(~104 C)
Jth: 670 A/cm2 at 300 K
Voltage efficiency: ~70%
Input power: 0.5 W
Max T: 33 C in cw
L. Li, Y. Jiang, et al., Appl. Phys. Lett.,106, 251102(2015)
Highlighted by Nature Photonics (2015)

## Slide 20: CW RT operation at λ=4.6-4.8 μm (2)
lowest Jth among diode lasers at similar wavelength
existing issues & future improvements:
NR device’s Jth ~50% larger than BA.
Better passivation to reduce leakage.
Rsth=6.5~11 Kcm2/kW, larger than 5.4 Kcm2/kW in GaSb-based IC laser.
Need to improve thermal dissipation.
vs. R125 (lasers w/t hybrid wg):
up to 40% improvement

## Slide 21: This work compare with others

## Slide 22: IC laser designed at λ=6.2-6.7 μm
Challenges | Solution
Reduced wavefunction overlap | new hole QW material ?
Reduced optical confinement | increase number of stages
Increased optical loss | hybrid waveguide, optimize doping

## Slide 23: Pulsed RT operation at λ=6.2-6.7 μm
Results comparable to best IC lasers by a competing group
 | this work | SPIE,9550,0F(2015)
Pulsed Jth at 300K | 810 A/cm2 (18 stages) | ~700 A/cm2 (22 stages)
T0 | 40 K | 41 K

## Slide 24: 2015 status of IC laser at λ> 6μm
CW RT to be achieved soon!
CW RT achieved in 2017!
Pulsed up to 357K
Jth (300K) = 333 A/cm2
Collaborated with NRC
Rassel, et al. Opt. Eng(2018)

## Slide 25: Electrically wide-tunable IC lasers
Why we need wide tuning:
spectroscopy
biochemical analysis
Tuning mechanisms:
Temperature tuning, based on Eg(T) or n(T)
cons: Slow
Grating tuning, such as external-cavity lasers
cons: Cumbersome, lack of long-term stability
Electric field tuning, based on the Stark effect
pros: responsive, convenient
challenge: electric field is difficult to change
after laser reaches threshold
solution: manipulate active region
Stark tuning:
?

## Slide 26: Electrically wide-tunable IC lasers
Stark tuning:
Solution 1:
Create different Jth by
multiple sections
Solution 2:
Shift gain-loss balance by
reducing Γ
increasing α
how to change N?

## Slide 27: Electrically wide-tunable IC lasers
Stark tuning:
Ze-h opposite to electric field direction -> blue-shift Stark tuning
Single QW
Double QWs

## Slide 28: Electrically wide-tunable IC lasers
Stark tuning:
Ze-h in the same direction with electric field -> red-shift Stark tuning
Triple QWs

## Slide 29: Electrically wide-tunable IC lasers
Stark tuning:
Solution 2:
Shift gain-loss balance by
reducing
increasing

## Slide 30: Electrically wide-tunable IC lasers
red-shifted by ~180 cm-1 (22 meV or 900 nm) around λ=7 μm
∆U= 3V, a strong evidence of carrier unpinning
small power efficiency, indicates small differential modal gain and high loss
Y. Jiang, et al., J. Appl. Phys., 115,113101(2014)
I also co-author in a patent of this design, approved in 2016

## Slide 31: GaSb-based type-I IC lasers at λ=3.2μm
carrier transition in type-I QW
carrier recycling in type-II QWs
Jth= 300 A/cm2 at pulsed 300K
6-stage cascade core, SL waveguide
material grown by NRC of Canada
Y. Jiang, et al., Appl. Phys. Lett., 106, 041117(2015)

## Slide 32: A detour after graduation
Why I paused MIR laser research:
  insufficient funding even before my graduation
  lack of security clearance for US IR laser industry
  NIR laser is more marketable than MIR. e.g. Hesai Photonics Technology (禾赛):Laser-Based Remote Methane Leak Detector
What I did in Weathernews:
  process geostationary satellite data using Python, C++ and Fortran
  built machine learning model using meteorological data (GFS, WRF, METAR), improving the productivity of aviation forecaster. (~ 20 forecasters cover ~360 Asian airports 7*24 hours)
  things learned: do we frame the question correctly and accurately?
  this detour is like a sabbatical leave, or a dropout scheme in the deep learning model, giving me fresh mind back to laser research
Notes: http://www.hesaitech.com/en/faq/laser.html?backUrl=/drone-mounted_natural_gas_surveillance_system.html
Capstone project: https://www.youtube.com/watch?v=w15GpupQusM

## Slide 33: My expertise
Design of laser active core and waveguide:
  focus on fundamentals  quickly pick up other types of lasers
  write Matlab codes from scratch: https://github.com/jychstar/interband_cascade_laser
Build testing setup and benchmark:
  suggest a rotation stage for far-field measurement
  suggest fabrication size & testing condition for cross comparison
  wrote Labview codes to get more precise data
  used lock-in amplifier to detect very small ASE signal
Design experiments to explain anomaly phenomena:
  temperature dependent P-I measurement for 11 um laser
  EL & Hakki-Paoli measurement for gain spectrum of 14 um laser

## Slide 34: What I can do for Hisense Photonics
Improve laser design by numerical simulation
Improve laser fabrication/packaging by empirical approach: trial-and-error, cost-efficiency analysis
Fully characterize laser and failure analysis at all stages
Automate data collection and processing
What I expect to learn in this position:
  What are customers’ specific needs?
  What are the industrial standard for a laser product?
  How to transit from research phase to mass production?
  What are potential research projects that can satisfy future’s application requirements

## Slide 35: Back up

## Slide 36: Waveguide variations
InAs Substrate
InAs Spacer
Cascade Stages
InAs Plasmon cladding n~3
InAs Spacer
Plasmon cladding
Contact
n=3.45
n=3.49
tunable refractive index
-> flexible waveguide design
plasmon
frequency
doping
concentration
symmetric cladding
asymmetric cladding
further simplify growth
easier to fabricate top DFB grating
Drude model

## Slide 37
基本结构和参数
SE-DFB-QCL结构示意图
各层掺杂浓度及折射率
基于耦合波模型的理论计算
激射波长：~ 4.7 µm
有效折射率：~3.16
周期：~1.48 µm
深度：~0.5 µm
占空比：？
室温设计

## Slide 38
器件后工艺
波长4.6 µm SE-DFB-QCL的制备
SiO2

## Slide 39
器件最终形貌
波长4.6 µm SE-DFB-QCL的制备
实际尺寸
周期：~1.48 µm
深度：~0.7 µm
占空比：25%

## Slide 40
光谱
波长4.6 µm SE-DFB-QCL的表征
单模，SMSR>15 dB，中心波长4.5748~4.6795 μm