## Slide 1: Interband Cascade Lasers: Current status and future work
Yuchao Jiang, PhD
2016.7.21

## Slide 2: Outline
Motivation and background
  Why interband cascade (IC) lasers?
  State-of-the-art IC lasers at λ~3.7 μm
My work: InAs-based IC lasers
  Single-mode DFB IC laser at λ=4.5 μm
  CW operation above RT at λ=4.6-4.8 μm
  Pulsed operation above RT at λ=6.2-6.7 μm
  Electrically widely tunable IC laser near λ=7 μm
My work: GaSb-based type-I IC lasers
  CW operation above RT at λ=3.2 μm
  High-frequency operation consisting of type-I IC laser and IC detector
Future work and ideas
  Achieve CW operation above RT at λ> 6μm
  Fundamental physics of the carrier transport in injection region
  Fundamental limits of T0 in any interband lasers

## Slide 3: why interband cascade (IC) lasers?
Mid-IR: 3-8 μm; Long-IR: 8~15 μm
Applications:
Gas-sensing
Free space optical
communications
So far, IC laser is the most efficient laser source in mid-wave IR range.
"Mars methane detection and variability at Gale crater", Science, 347, 415 (2015).

## Slide 4: Why interband cascade (IC) lasers? vs. non-cascade interband lasers
Shared issues for any interband lasers:
free carrier absorption loss
Auger recombination dominates Jth(=e∙nth/ τ)
Advantages of cascade structure :
reduce nth-> reduce Auger
like power transmission line -> lower ohmic loss
R. Yang, S. Pei, J. Appl. Phys. 79,8197(1996)
 | type | equivalent circuit | key difference
a | MQW laser | in parallel | low voltage
b | IC laser | in series | low current
GaN LED in a cascade style overcame(?) efficiency droop.
F. Akyol, et al., Appl. Phys. Lett. 103,081107(2013)

## Slide 5: Why interband cascade (IC) lasers? vs. quantum cascade (QC) lasers
Only two technologies capable of CW RT in mid-IR
 | QC laser | IC laser
material system | InGaAs/InAlAs/InP | InAs/GaSb/AlSb
carrier transition, lifetime | inter-subband, ~1 ps | interband, ~1 ns
threshold current density | 860 A/cm2 @4.6μm | 100 A/cm2 @3.6μm
threshold voltage | 12.8 V (40 stages) | 3 V (10 stages)
threshold power density | 11 kW/cm2 | 0.3 kW/cm2
maximum output power | 5.1 W | 0.6 W
thermal conductivity | InP: 68 W/m∙K | GaSb:33; InAs:27
IC laser is a better solution for battery powered applications.
ref: APL, 95,141113 (2009) ; APL, 102,231123(2013)
APL, 89,181102 (2011); Opt Exp., 22,7702(2014)

## Slide 6: Snapshot of IC laser development
How the progress is made?
better material & fabrication
improved understanding & design
trial and error

## Slide 7: Band structure of IC laser
“Rebalancing of internally generated carriers for mid-infrared interband cascade lasers with very low power consumption”,
Vurgaftman, et al., Nature Communication, 2, 585 (2011)
bias
Design innovations since the prototype by R. Yang in 1994:
“W” like active region
2 QWs in hole injector
fine tune barrier thickness
semi-metallic interface
shortened electron injector
“carrier rebalancing”
(not fully understood)

## Slide 8: Waveguide structures of IC lasers
Material | Thermal Conductivity
InAs/AlSb SL | ~ 2.7 W/m·K
InAs | ~ 27 W/m·K
GaSb | ~ 33 W/m·K
Better thermal dissipation
Simplify the growth
Tunable refractive index
GaSb Substrate
GaSb Spacer
Cascade Stages
InAs/AlSb SL n=3.35
GaSb Spacer
InAs/AlSb SL
Contact
n=3.45
n=3.73
InAs Substrate
InAs Spacer
Cascade Stages
InAs n++ n~3
InAs Spacer
InAs n++
Contact
n=3.45
n=3.49
InAs-based IC lasers may be
a better solution at longer λ
top cladding
bottom
cladding
InAs Plasmon-Enhanced Waveguide
InAs/AlSb Superlattice Waveguide

## Slide 9: Why InAs-based IC lasers?
InAs Substrate
InAs Spacer
Cascade Stages
InAs Plasmon cladding n~3
InAs Spacer
Plasmon cladding
Contact
n=3.45
n=3.49
tunable refractive index
-> flexible waveguide design
plasmon
frequency
doping
concentration
symmetric cladding
asymmetric cladding
further simplify growth
easier to fabricate top DFB grating
Drude model

## Slide 10: Real device & testing set-up
Cascade stages
Top spacer
Bottom spacer
1 μm
Side
view
200 μm
Laser mesa
Trench
Cryostat
sensor A
Vacuum
LN2
Temperature
Controller
sensor B
heater
Laser
Current in
Light
out
Semiconductor grating

## Slide 11: InAs-based Single-mode DFB IC laser
Single frequency-mode laser is desirable for gas-sensing
First DFB IC laser with an asymmetric waveguide
Y. Jiang, et al., IEEE J. Quantum Electron. 51, 2300307(2015)

## Slide 12: Laser design by threshold analysis
Modal gain (measurable)
Confinement factor
of Active QWs
Material gain (unmeasurable)
End goal: minimize threshold:
Design approaches:
Active core optimization (future work)
Optical waveguide optimization (current work)

## Slide 13: Optical waveguide optimization(1)
plasmon
frequency
doping
concentration
Drude model
When λemission near λplasmon:
n decreases sharply
loss increase exponentially

## Slide 14: Optical waveguide optimization(2)
Plasmon waveguide
requires higher
material gain!

## Slide 15: Optical waveguide optimization(3)
Hybrid waveguide:
InAs spacer layer
InAs/AlSb SL inner cladding
InAs plasmon outer cladding
Predict threshold gain
reduced by ~30%

## Slide 16: CW RT operation at λ=4.6-4.8 μm (1)
Max pulsed operation
temperature: 377 K(~104 C)
Jth: 670 A/cm2 at 300 K
Voltage efficiency: ~70%
Input power: 0.5 W
Max T: 33 C in cw
L. Li, et al., Appl. Phys. Lett.,106, 251102(2015)

## Slide 17: CW RT operation at λ=4.6-4.8 μm (2)
lowest Jth among diode lasers at similar wavelength
existing issues & future improvements:
NR device’s Jth ~50% larger than BA.
Better passivation to reduce leakage.
Rsth=6.5~11 Kcm2/kW, larger than 5.4 Kcm2/kW in GaSb-based IC laser.
Need to improve thermal dissipation.
vs. R125 (lasers w/t hybrid wg):
up to 40% improvement

## Slide 18: This work compare with others

## Slide 19: IC laser designed at λ=6.2-6.7 μm
Challenges | Solution
Reduced wavefunction overlap | new hole QW material ?
Reduced optical confinement | increase number of stages
Increased optical loss | hybrid waveguide, optimize doping

## Slide 20: Pulsed RT operation at λ=6.2-6.7 μm
Results comparable to best IC lasers by a competing group
 | this work | SPIE,9550,0F(2015)
Pulsed Jth at 300K | 810 A/cm2 (18 stages) | ~700 A/cm2 (22 stages)
T0 | 40 K | 41 K

## Slide 21: Current status of IC laser at λ> 6μm
CW RT to be achieved soon!

## Slide 22: Electrically wide-tunable IC lasers (1)
Why we need wide tuning:
spectroscopy
biochemical analysis
Tuning mechanisms:
Temperature tuning, based on Eg(T) or n(T)
cons: Slow
Grating tuning, such as external-cavity lasers
cons: Cumbersome, lack of long-term stability
Electric field tuning, based on the Stark effect
pros: responsive, convenient
challenge: electric field is difficult to change
after laser reaches threshold
solution: manipulate active region
Stark tuning:
?

## Slide 23: Electrically wide-tunable IC lasers (2)
Stark tuning:
Solution 1:
Create different Jth by
multiple sections
Solution 2:
Shift gain-loss balance by
reducing Γ
increasing α
how to change N?

## Slide 24: Electrically wide-tunable IC lasers (3)
Stark tuning:
Ze-h opposite to electric field direction -> blue-shift Stark tuning
Single QW
Double QWs

## Slide 25: Electrically wide-tunable IC lasers (4)
Stark tuning:
Ze-h in the same direction with electric field -> red-shift Stark tuning
Triple QWs

## Slide 26: Electrically wide-tunable IC lasers (5)
Stark tuning:
Solution 2:
Shift gain-loss balance by
reducing
increasing

## Slide 27: Electrically wide-tunable IC lasers (6)
red-shifted by ~180 cm-1 (22 meV or 900 nm) around λ=7 μm
∆U= 3V, a strong evidence of carrier unpinning
small power efficiency, indicates small differential modal gain and high loss
Y. Jiang, et al., J. Appl. Phys., 115,113101(2014)

## Slide 28: Electrically wide-tunable IC lasers (7)
∆U=2.44 V
Stark effect dominate over heating effect

## Slide 29: GaSb-based type-I IC lasers at λ=3.2μm
carrier transition in type-I QW
carrier recycling in type-II QWs
Jth= 300 A/cm2 at pulsed 300K
6-stage cascade core, SL waveguide
material grown by NRC of Canada
Y. Jiang, et al., Appl. Phys. Lett., 106, 041117(2015)

## Slide 30: High-speed operation
H. Lotfi, et al., APL, 108, 201101(2016)

## Slide 31: Future work & ideas (1)
Vurgaftman, et al., Nat. Commun., 2, 585 (2011)
Is “carrier rebalancing” true?
is more an experimental finding
explained as electron-hole balance in active region
 | doping | Jth
conventional | 4e17 cm-3 | 380 A/cm2
innovation | 5e18 cm-3 | 167 A/cm2
Not really
scanning voltage microscopy shows the electron
and hole densities are always equal in active region
no matter which doping. [Laser Photon. Rev. 2,224(2015)]
the optimal doping is found by fitting Auger coefficient,
not by more fundamental parameters.

## Slide 32: “carrier rebalancing”?
my insights:
It is because the imbalance of
electron and hole effective mass
heavy doping facilitate the Bernard-
Duraffourg inversion condition, so as
reduce transparence carrier density
Optimal doping is on the order of
effective density of states Nc
will need more accurate modeling
and systematical experiments to verify
my idea.

## Slide 33: Future work & ideas (2) why small T0 in most interband lasers?
Jth=J0exp(T/T0) is widely used to characterize the temperature sensitivity of diode lasers, but T0 is always much smaller than room temperature.
This affects the practical use of laser. A deeper understanding of the origin of small T0 will be very meaningful.
I have some initial results by:
first principle calculation of
the gain coefficient
empirical data of optical loss
and Auger coefficient
need more complete data to achieve
a more comprehensive model

## Slide 34: Future work & ideas (3) why internal efficiency <1 after lasing?
Ideally, carrier density is pinned at threshold level after lasing, so the internal efficiency should be very close to unity.
But in reality, the efficiency is far from unity.
At high injection, the laser stop working, even at pulsed operation.
possible factors:
increased loss
thermal accumulation
carrier leakage