## Slide 1: Presentation at Hisense Photonics
Yuchao Jiang, PhD
2018.12.10

## Slide 2: Outline
Educational background
Past research experience
A detour in career
What I can do for HiSense Photonics

## Slide 3: Educational Background
Born in FuJian(福建).
2007, B.S., Applied Physics.
2010. M.S., Material Physics.
2016. Ph.D. in Electrical & Computer Engineering.

## Slide 4: My research experience
InP-based Quantum Cascade (QC) Lasers
  Surface-emitting DFB QC lasers at λ ~ 4.6 µm
InAs-based Interband Cascade (IC) lasers
  Single-mode DFB IC laser at λ=4.5 μm
  CW operation above RT at λ=4.6-4.8 μm
  Pulsed operation above RT at λ=6.2-6.7 μm
  Electrically widely tunable IC laser near λ=7 μm
GaSb-based type-I IC lasers
  CW operation above RT at λ=3.2 μm

## Slide 5: Why interband cascade (IC) lasers?
Mid-IR: 3-8 μm; Long-IR: 8~15 μm
Applications:
Gas-sensing
(ppb-level trace gas)
Free space optical communications
Highly energy efficient! 1/10 of competitor (QC laser).
Using iPhone 6 battery (10.5 Wh) can work ~50 hours.
Launch: 2011.11.26
Landing: 2012.8.6

## Slide 6: Methane on Mars? No?
One year after landing…
Notes: Sensing methane is difficult

## Slide 7: Methane on Mars? Yes!
Another year passes…
1 Mars year = 687 earth days
1 Mars day = 1 earth day + 41 min
Notes: https://mars.nasa.gov/allaboutmars/facts/#?c=inspace&s=distance

## Slide 8: Why interband cascade (IC) lasers? vs. non-cascade interband lasers
Shared issues for any interband lasers:
free carrier absorption loss
Auger recombination dominates Jth(=e∙nth/ τ)
Advantages of cascade structure :
reduce nth-> reduce Auger
Analogy: power transmission line -> lower ohmic loss
R. Yang, S. Pei, J. Appl. Phys. 79,8197(1996)
 | type | equivalent circuit | key difference
a | MQW laser | in parallel | low voltage
b | IC laser | in series | low current
GaN LED in a cascade style overcame efficiency droop.
F. Akyol, et al., Appl. Phys. Lett. 103,081107(2013)

## Slide 9: Why interband cascade (IC) lasers? vs. quantum cascade (QC) lasers
Only two technologies capable of CW RT in mid-IR
 | QC laser | IC laser
material system | InGaAs/InAlAs/InP | InAs/GaSb/AlSb
carrier transition, lifetime | inter-subband, ~1 ps | interband, ~1 ns
threshold current density | 860 A/cm2 @4.6μm | 100 A/cm2 @3.6μm
threshold voltage | 12.8 V (40 stages) | 3 V (10 stages)
threshold power density | 11 kW/cm2 | 0.3 kW/cm2
maximum output power | 5.1 W | 0.6 W
thermal conductivity | InP: 68 W/m∙K | GaSb:33; InAs:27
IC laser is a better solution for battery powered applications.
ref: APL, 95,141113 (2009) ; APL, 102,231123(2013)
APL, 89,181102 (2011); Opt Exp., 22,7702(2014)

## Slide 10: Snapshot of IC laser development
How the progress is made?
better material & fabrication
improved understanding & design
trial and error

## Slide 11: Real device & testing set-up
Cascade stages
Top spacer
Bottom spacer
1 μm
Side
view
200 μm
Laser mesa
Trench
Cryostat
sensor A
Vacuum
LN2
Temperature
Controller
sensor B
heater
Laser
Current in
Light
out
Semiconductor grating

## Slide 12: InAs-based Single-mode DFB IC laser
Single frequency-mode laser is desirable for gas-sensing
First DFB IC laser with an asymmetric waveguide
Y. Jiang, et al., IEEE J. Quantum Electron. 51, 2300307(2015)

## Slide 13: Laser design by threshold analysis
Modal gain (measurable)
Confinement factor
of Active QWs
Material gain (unmeasurable)
End goal: minimize threshold:
Design approaches:
Active core optimization (future work)
Optical waveguide optimization (current work)

## Slide 14: Band structure of IC laser
“Rebalancing of internally generated carriers for mid-infrared interband cascade lasers with very low power consumption”,
Vurgaftman, et al., Nature Communication, 2, 585 (2011)
bias
Design innovations since the prototype by R. Yang in 1994:
“W” like active region
2 QWs in hole injector
fine tune barrier thickness
semi-metallic interface
shortened electron injector
“carrier rebalancing”
(not fully understood)

## Slide 15: Waveguide structures of IC lasers
Material | Thermal Conductivity
InAs/AlSb SL | ~ 2.7 W/m·K
InAs | ~ 27 W/m·K
GaSb | ~ 33 W/m·K
Better thermal dissipation
Simplify the growth
Tunable refractive index
GaSb Substrate
GaSb Spacer
Cascade Stages
InAs/AlSb SL n=3.35
GaSb Spacer
InAs/AlSb SL
Contact
n=3.45
n=3.73
InAs Substrate
InAs Spacer
Cascade Stages
InAs n++ n~3
InAs Spacer
InAs n++
Contact
n=3.45
n=3.49
InAs-based IC lasers may be
a better solution at longer λ
top cladding
bottom
cladding
InAs Plasmon-Enhanced Waveguide
InAs/AlSb Superlattice Waveguide

## Slide 16: Optical waveguide optimization(1)
plasmon
frequency
doping
concentration
Drude model
When λemission near λplasmon:
n decreases sharply
loss increase exponentially

## Slide 17: Optical waveguide optimization(2)
Plasmon waveguide
requires higher
material gain!

## Slide 18: Optical waveguide optimization(3)
Hybrid waveguide:
InAs spacer layer
InAs/AlSb SL inner cladding
InAs plasmon outer cladding
Predict threshold gain
reduced by ~30%

## Slide 19: CW RT operation at λ=4.6-4.8 μm (1)
Max pulsed operation
temperature: 377 K(~104 C)
Jth: 670 A/cm2 at 300 K
Voltage efficiency: ~70%
Input power: 0.5 W
Max T: 33 C in cw
L. Li, Y. Jiang, et al., Appl. Phys. Lett.,106, 251102(2015)
Highlighted by Nature Photonics (2015)

## Slide 20: CW RT operation at λ=4.6-4.8 μm (2)
lowest Jth among diode lasers at similar wavelength
existing issues & future improvements:
NR device’s Jth ~50% larger than BA.
Better passivation to reduce leakage.
Rsth=6.5~11 Kcm2/kW, larger than 5.4 Kcm2/kW in GaSb-based IC laser.
Need to improve thermal dissipation.
vs. R125 (lasers w/t hybrid wg):
up to 40% improvement

## Slide 21: This work compare with others

## Slide 22: IC laser designed at λ=6.2-6.7 μm
Challenges | Solution
Reduced wavefunction overlap | new hole QW material ?
Reduced optical confinement | increase number of stages
Increased optical loss | hybrid waveguide, optimize doping

## Slide 23: Pulsed RT operation at λ=6.2-6.7 μm
Results comparable to best IC lasers by a competing group
 | this work | SPIE,9550,0F(2015)
Pulsed Jth at 300K | 810 A/cm2 (18 stages) | ~700 A/cm2 (22 stages)
T0 | 40 K | 41 K

## Slide 24: 2015 status of IC laser at λ> 6μm
CW RT to be achieved soon!
CW RT achieved in 2017!
Pulsed up to 357K
Jth (300K) = 333 A/cm2
Collaborated with NRC
Rassel, et al. Opt. Eng(2018)

## Slide 25: Electrically wide-tunable IC lasers
Why we need wide tuning:
spectroscopy
biochemical analysis
Tuning mechanisms:
Temperature tuning, based on Eg(T) or n(T)
cons: Slow
Grating tuning, such as external-cavity lasers
cons: Cumbersome, lack of long-term stability
Electric field tuning, based on the Stark effect
pros: responsive, convenient
challenge: electric field is difficult to change
after laser reaches threshold
solution: manipulate active region
Stark tuning:
?

## Slide 26: Electrically wide-tunable IC lasers
Stark tuning:
Solution 1:
Create different Jth by
multiple sections
Solution 2:
Shift gain-loss balance by
reducing Γ
increasing α
how to change N?

## Slide 27: Electrically wide-tunable IC lasers
Stark tuning:
Ze-h opposite to electric field direction -> blue-shift Stark tuning
Single QW
Double QWs

## Slide 28: Electrically wide-tunable IC lasers
Stark tuning:
Ze-h in the same direction with electric field -> red-shift Stark tuning
Triple QWs

## Slide 29: Electrically wide-tunable IC lasers
Stark tuning:
Solution 2:
Shift gain-loss balance by
reducing
increasing

## Slide 30: Electrically wide-tunable IC lasers
red-shifted by ~180 cm-1 (22 meV or 900 nm) around λ=7 μm
∆U= 3V, a strong evidence of carrier unpinning
small power efficiency, indicates small differential modal gain and high loss
Y. Jiang, et al., J. Appl. Phys., 115,113101(2014)

## Slide 31: GaSb-based type-I IC lasers at λ=3.2μm
carrier transition in type-I QW
carrier recycling in type-II QWs
Jth= 300 A/cm2 at pulsed 300K
6-stage cascade core, SL waveguide
material grown by NRC of Canada
Y. Jiang, et al., Appl. Phys. Lett., 106, 041117(2015)

## Slide 32: A detour after graduation
factors affecting me pausing MIR laser research:
  insufficient funding even before my graduation
  lack of security clearance for US IR laser industry
  NIR laser is more marketable than MIR. e.g. Hesai Photonics Technology (禾赛):Laser-Based Remote Methane Leak Detector
A dive into this 3rd AI wave:
  a probability/statistical approach to digest huge data
  bottlenecks: black box, expensive (robotic arms, lidar)
  rethink the fundamentals in a hyper-information age
  Do we frame the question correctly and accurately?
Notes: http://www.hesaitech.com/en/faq/laser.html?backUrl=/drone-mounted_natural_gas_surveillance_system.html
Capstone project: https://www.youtube.com/watch?v=w15GpupQusM

## Slide 33: What I can do for Hisense Photonics
Improve laser design from theoretical and practical way
Fully characterize laser and failure analysis at all stages
Automate data collection and processing
Assist transition from research phase to mass production
Clarify customer's specific needs and provide solutions
Research for novel lasers and system integration to satisfy future’s requirement

## Slide 34: Back up

## Slide 35: Waveguide variations
InAs Substrate
InAs Spacer
Cascade Stages
InAs Plasmon cladding n~3
InAs Spacer
Plasmon cladding
Contact
n=3.45
n=3.49
tunable refractive index
-> flexible waveguide design
plasmon
frequency
doping
concentration
symmetric cladding
asymmetric cladding
further simplify growth
easier to fabricate top DFB grating
Drude model

## Slide 36
基本结构和参数
SE-DFB-QCL结构示意图
各层掺杂浓度及折射率
基于耦合波模型的理论计算
激射波长：~ 4.7 µm
有效折射率：~3.16
周期：~1.48 µm
深度：~0.5 µm
占空比：？
室温设计

## Slide 37
器件后工艺
波长4.6 µm SE-DFB-QCL的制备
SiO2

## Slide 38
器件最终形貌
波长4.6 µm SE-DFB-QCL的制备
实际尺寸
周期：~1.48 µm
深度：~0.7 µm
占空比：25%

## Slide 39
光谱
波长4.6 µm SE-DFB-QCL的表征
单模，SMSR>15 dB，中心波长4.5748~4.6795 μm