## Slide 1: Interband cascade structures for infrared photodetectors and thermophotovoltaic devices
Hossein Lotfi
Ph.D. oral presentation
December 08, 2016

## Slide 2
Outline
Background and motivations
Interband cascade devices: principles of operation
HOT long- and very long-wavelength ICIPs
High-performance short-wavelength ICIPs
High-frequency interband cascade systems
Monolithically integrated mid-IR laser and detector
Interband cascade thermophotovoltaic devices
Summary and research perspective

## Slide 3
Outline
Background and motivations
Interband cascade devices: principles of operation
HOT long- and very long-wavelength ICIPs
High-performance short wavelength ICIPs
High-frequency interband cascade systems
Monolithically integrated mid-IR laser and detector
Interband cascade thermophotovoltaic devices
Summary and research perspective

## Slide 4
Background and motivations
Image source: JPL
Free space communication
Thermophotovoltaic devices
Data from: HITRAN
Molecule and gas sensing
Thermal imaging
Tian et al, Appl. Phys. Lett. 2014

## Slide 5
Interband cascade (IC) devices: background
Family of IC devices:
Interband cascade lasers
Interband cascade IR photodetectors
Interband cascade photovoltaic devices
6.1 Å material family

## Slide 6
The electron and hole wave functions are spatially located in the same layer
The electron and hole wave functions are spatially located in different layers
Type-I vs. type-II quantum wells

## Slide 7
Outline
Background and Motivations
Interband cascade devices: principles of operation
HOT long- and very long-wavelength ICIPs
High-performance short wavelength ICIPs
High-frequency interband cascade systems
Monolithically integrated mid-IR laser and detector
Interband cascade thermophotovoltaic devices
Summary and research perspective

## Slide 8
Interband cascade lasers
multiple photons per electron
Benefits of cascade lasers:
High efficiency
Large output power
Uniform carrier injection in every stage
Low carrier concentration
carrier injection
hv
hv
hv
carrier extraction
active region
active region
active region
interband
tunneling
interband
tunneling
(Type-II QWs)
(Type-II QWs)

## Slide 9
Interband cascade IR photodetectors
Ee
Eh
hv
E
e
interband
tunneling
SL
absorber
intraband
relaxation
intraband
relaxation
hν
QWs
with
type-II
hetero-interface
hv
(1)
(2)
(3)
e
e
excitation
SL
absorber
QWs
with
type-II
hetero-interface
hole barrier
electron barrier
hole barrier
hole barrier
electron barrier
(1)
(2)
(3)
(2)
one interband cascade stage – double heterostructure unit
digitally graded AlSb/InAs QWs
InAs/GaSb SL
GaSb/AlSb QWs
hv
hv
hv
hv
hv
hv
hv
multiple photons are required to output one electron
hv
hv
hv
hv
E
e
ICL vs. ICIP

## Slide 10: Different configurations for ICIPs
Regular configuration
Reverse configuration
Early ICIPs had regular configuration
Electron barrier is located at the top and
hole barrier is located at the bottom of each
stage
Electrons need to diffuse a longer distance
Hole barrier located at the top and
electron barrier is located at the bottom of
each stage
Electrons are populated closer to the
collection point

## Slide 11: High-operating-temperature (HOT) IR detectors
Thick absorbers are required to ensure enough photon absorption (large QE)
Problems:
Decreased diffusion length at high temperatures
Very small device resistance
Large dark currents and large noise
Long carrier transit time
Solution:
R. T. Hinkey and R. Q. Yang, Proc. SPIE 8868, (2013)

## Slide 12: Multiple stages vs. single stage
R1
R2
RN
ICIP
single-absorber detector
Absorber thickness: Lsing=N·L
Absorber resistance → R/N
Response: NRλ
Absorber resistance → NR
Response: Rλ
D* is a measure of signal to noise ratio
D*
Where are the benefits of ICIPs?

## Slide 13: Single vs. multiple stages: detectivity
R. T. Hinkey and R. Q. Yang, Journal of Applied Physics, (2013)

## Slide 14
MBE growth and device fabrication

## Slide 15
Outline
Background and Motivations
Interband cascade devices: principles of operation
HOT long- and very long-wavelength ICIPs
High-performance short wavelength ICIPs
High-frequency interband cascade systems
Monolithically integrated mid-IR laser and detector
Interband cascade thermophotovoltaic devices
Summary and research perspective

## Slide 16: HOT long-wavelength ICIPs
Three ICIPs with identical unipolar barriers and absorber’s SL period
Goal: to investigate the effects of different number of stages and illumination direction on device performance

## Slide 17: Long-wavelength ICIPs
XRD measurements: similar interface and material quality in the three wafers
EL measurements: two wafers had similar structural and interface quality, while wafer Reg.-2S may have somewhat better optical properties.

## Slide 18: Long-wavelength ICIPs
The measured dark currents did not follow the theory of ideal ICIPs at low temperatures
The material growth and/or device fabrication variations from one wafer to another

## Slide 19: Long-wavelength ICIPs
Lower responsivity in the three-stage ICIPs (10% at λ=5 μm)
Larger detectivity in the three-stage ICIPs at 125 K and above
Rev.-2s had poor electrical and optical performance low D*
λ=5 μm

## Slide 20: Very long-wavelength (λc=16 μm) ICIPs
Three photo-current ICIP with
reverse configuration
Dark current density at 78 K and 50 mV:
One-stage device: 100 mA/cm2
Three-stage ICIP: 25 mA/cm2
Two-stage ICIP: 24 mA/cm2

## Slide 21: Very long-wavelength ICIPs
The zero-bias responsivity was low in the VLWIR wafers
The zero-bias responsivity increased with temperature
These observations support the existence of an unwanted electrostatic barrier

## Slide 22
Outline
Background and Motivations
Interband cascade devices: principles of operation
HOT long- and very long-wavelength ICIPs
High-performance short wavelength ICIPs
High-frequency interband cascade systems
Monolithically integrated mid-IR laser and detector
Interband cascade thermophotovoltaic devices
Summary and research perspective

## Slide 23: Short-wavelength ICIPs
Two-stage
Three-stage
Cutoff wavelength: 2.8 μm

## Slide 24: Device performance: dark current
Dark current was lower in three-stage ICIPs compared to two-stage ICIPs
Size dependent dark current densities were observed in both wafers
Lotfi, et al., Journal of Applied Physics (2016)

## Slide 25: Device performance: optical
Lower responsivity in the three-stage ICIPs (16%)
Larger detectivity in the three-stage ICIPs
There is room for improvements

## Slide 26
Diffusion length estimation
Larger set of detectors decreases the uncertainty
Specific designs will have larger margins
Bulk R0A, no surface currents
Diffusion limited transport
Uniform material and fabrication
450 nm
350 nm
≤170 nm
300 K
320 K
340 K
Exp.

## Slide 27
Outline
Background and Motivations
Interband cascade devices: principles of operation
HOT long- and very long-wavelength ICIPs
High-performance short wavelength ICIPs
High-frequency interband cascade systems
Monolithically integrated mid-IR laser and detector
Interband cascade thermophotovoltaic devices
Summary and research perspective

## Slide 28
Single vs. multiple stages: speed
R1
R2
RN
ICIP
single-absorber detector
Absorber thickness: Lsing=N·L
Absorber resistance → R/N
Response: NRλ
Absorber resistance → NR
Response: Rλ
Shorter absorbers reduce the transit time → high-speed operation
Higher speed with the same detectivity

## Slide 29: Device structure and characteristics
Devices with different number of stages and absorbers were grown
Three-stage ICIP with reverse configuration:

## Slide 30: High-frequency modulation setup

## Slide 31: System performance: circuit model
System BW:
850 MHz
ICL BW:
760 MHz
ICIP BW:
1.3 GHz

## Slide 32
Single- and multiple stage ICIPs had similar (3.1 μm) total absorber thickness
Both detectors had similar zero-bias normalized detectivities (~1×109 cmHz1/2/W)
Bit rate of 48 Mb/s
eight stage
one stage, absorber: 1 mm
Single vs. multiple stage ICIP

## Slide 33
Input bits to an IC laser
Inverted output bits from an ICIP
R146 (50×50 μm2)
100 ns per division
Input and Output Bit Sequence
0 0 0 0 0 11 00 1 0 11 0 11

## Slide 34
Free space optical communication link

## Slide 35
Outline
Background and Motivations
Interband cascade devices: principles of operation
HOT long- and very long-wavelength ICIPs
High-performance short wavelength ICIPs
High-frequency interband cascade systems
Monolithically integrated mid-IR laser and detector
Interband cascade thermophotovoltaic devices
Summary and research perspective

## Slide 36
Monolithically integrated mid-IR laser and detector
Base structure: type-I ICL with six-stages and GaInAsSb active regions
Focused ion beam (FIB) milling was employed to define each ICLD unit

## Slide 37
Monolithically integrated mid-IR laser and detector
Opens new horizons for high-performance miniaturized mid-IR systems
Short-circuit current (Isc) ~106 μA
Open-circuit voltage (Voc) ~ 1.06 V >> Eg/e=0.38 V (cascade action)
Projected D*: ~1.85×1010 cm.Hz1/2/W at 20 ◦C

## Slide 38
Outline
Background and Motivations
Interband cascade devices: principles of operation
HOT long- and very long-wavelength ICIPs
High-performance short wavelength ICIPs
High-frequency interband cascade systems
Monolithically integrated mid-IR laser and detector
Interband cascade thermophotovoltaic devices
Summary and research perspective

## Slide 39
Interband cascade thermophotovoltaic devices
Harvest energy from thermal sources: solar, nuclear, waste heat
Heat sources from 1000 K to 2000 K
Optimum bandgap: 0.2 - 0.4 eV

## Slide 40
Interband cascade thermophotovoltaic devices
Circumvent the diffusion length limitation  High collection efficiency
InAs/GaSb SL
Hole
Barrier
Electron
Barrier
Absorber
Eh
Electron flow
Hole flow
InAs/GaSb SL
Hole
Barrier
Absorber
Eh
Ee
Electron flow
Hole flow
Ee
Photons
Electron
Barrier
Hole
Barrier
InAs/GaSb SL
Absorber
Eh
Ee
Electron flow
Hole flow
Electron
Barrier
one cascade stage

## Slide 41
Interband cascade thermophotovoltaic devices
EQE was larger in twos-ate compared to three-stage devices
Three-stage
Two-stage

## Slide 42
Interband cascade thermophotovoltaic devices
An IC laser used to mimic a selective emitter
Four wire setup: to reduce the parasitic resistances influence at high illumination levels

## Slide 43
Interband cascade thermophotovoltaic devices
T (K) | Jsc (A/cm2) | Iph (mA) | Voc (mV) | Rs (Ω) | Rsh (kΩ) | FF (%)
300 | 50.0 | 21.0 | 509 | 9.27 | 5.04 | 47.5
340 | 53.6 | 23.5 | 445 | 8.67 | 0.85 | 40.7
T (K) | Jsc (A/cm2) | Iph (mA) | Voc (mV) | Rs (Ω) | Rsh (Ω) | FF (%)
300 | 43.5 | 17.9 | 799 | 12.14 | 9.04 | 51.4
340 | 48.4 | 20.8 | 666 | 11.09 | 1.38 | 44.9

## Slide 44
Interband cascade thermophotovoltaic devices
Conversion efficiency:
Two-stage: 6.5 % Three-stage: 9.6 %
The device efficiency exhibited a roll off at high illumination levels

## Slide 45
Interband cascade thermophotovoltaic devices
Series resistance was larger in three-stage devices
Larger bulk series resistance due to extra absorber
Non-ideal Ohmic contacts
Unwanted electrostatic barrier in carrier transport path
An effective characterization method (based on Suns-Voc technique) for extracting series and shunt resistances was developed

## Slide 46
Interband cascade thermophotovoltaic devices
Narrow-bandgap ICTPV devices with seven identical stages
The cutoff wavelength: 5 μm at 300 K and 5.2 μm at 340 K
Relatively low QE:
~31% reflection loss from the air/semiconductor interface
Short overall absorber thickness (~1.1 μm total from seven stages)

## Slide 47
Interband cascade thermophotovoltaic devices
Device performance metrics at 300 K
The highest FF: 43% with illumination of a laser near 4.3 μm
Pmax: 395 mW/cm2 at an incident laser power density of 18.9 W/cm2
Power conversion efficiency: 2.1%

## Slide 48
Outline
Background and Motivations
Interband cascade devices: principles of operation
HOT long- and very long-wavelength ICIPs
High-performance short wavelength ICIPs
High-frequency interband cascade systems
Monolithically integrated mid-IR laser and detector
Interband cascade thermophotovoltaic devices
Summary and research perspective

## Slide 49
Summary and research perspective
ICIPs are unique structures for HOT and high-speed applications
First demonstration of HOT LWIR and VLWIR ICIPs was discussed
Short-wave ICIPs with three stages had better performance,
there is room for further improvements
Diffusion length seems to be significantly shorter than
a typical absorber in conventional IR detectors
An uncooled high-speed (f3dB850 MHz) IC system is demonstrated
Monolithically integrated laser and detector units open new horizons
for on chip spectrometers, lab-on-a chip devices and on-chip
communication
ICTPVs with efficiencies of ~10 % were demonstrated

## Slide 50
Acknowledgements
Prof. Rui Q. Yang (advisor)
Prof. Matthew B. Johnson
Prof. Michael B. Santos
Dr. Robert T. Hinkey
Dr. Lu Li
Dr. Hao Ye
S. M. Shazzad Rassel
Lin Lei
Dr. Yuchao Jiang
Dr. John F. Klem of Sandia National Laboratories
Dr. James A. Gupta of National Research Council of Canada
Drs. Yueming Qiu, Dmitri Lubyshev, Joel M. Fastenau, and Amy W. K. Liu of IQE Inc.
Dr. Preston R. Larson
Cédric J. Corrége
Dr. Joel C. Keay
Dr. Tetsuya D. Mishima
Profs. Zhisheng Shi, J. R. Cruz and Ian R. Sellers
Wenxiang Huang
Lihua Zhao
And my wife, friends and family
The research presented in this dissertation was supported by funding from DoE EPSCoR program
(Award No. DE-SC0004523), C-SPIN, the Oklahoma/Arkansas MRSEC (Award No. DMR- 0520550),
AFOSR (Award No. FA9550-12-1-0260), NSF (Award No. ECCS-1202318),
AFOSR (Award No. FA9550-15-1- 0067), NSF (Award No. DMR-1229678),
and NSF (Award No. DMR-1608224).

## Slide 51: Thank You!

## Slide 52: Backup

## Slide 53: Long-wavelength ICIPs
Stage 1
Stage 2
Two-stage ICIPs with cutoff wavelength of ~ 9.2 μm (78 K)
Absorber 1: 620 nm
Absorber 2: 756.4 nm

## Slide 54: Long-wavelength ICIPs
Bias dependent response at high temperatures (167 K and above):
Decreased diffusion length
Switching of the residual doping from p-type to n-type
D*: 3.7×1010 cm.Hz1/2/W at 78 ◦K
Best D* for ICIPs of similar wavelength: 1.3×1011 cm.Hz1/2/W
See J. Appl. Phys. 120, 193102 (2016).

## Slide 55: Suns-Voc technique

## Slide 56: Some math on ICIPs

## Slide 57: Absorption and diffusion length